Characteristics of Hydrochar generated from Food Waste

Min-Seon Choi and Sunyoung Bae *

Department of Chemistry, Seoul Women’s University, Nowon-gu Hwarang-ro, Seoul 621, Korea

Introduction and Results:

Hydrochar has been received much attention due to the potential of carbon sequestration, the improvement of soil quality, and the sorption capacity of pollution such as heavy metals. Hydrochar is generated by hydrothermal carbonization reaction (HTC). It is proven as a novel thermal conversion process using biomass. Characterization of physicochemical properties may determine the sorption capacity such as sorption of heavy metals. Particularly, the surface characteristics would control the sorption patterns and mechanism on the hydrochar. In this study, production of hydrochar was optimized by varying HTC conditions (Reaction temperature : 220 oC, 230 oC, Reaction time : 1 h, 2 h, 4 h, 6 h, 8 h). The optimum condition of hydrochar production was determined based on iodine number and methylene blue number comparing with BET measurements. The optimum condition of hydrochar production was determined at 230 oC for 4 hr. The further functional groups were identified by using FT-IR, SEM and Boehm titration. To identify the sorption capacity of hydrochar applied in soil, Pb solution of 2, 5, 8, 10 ppm was applied to soil mixed with hydrochar at the ratio of 0, 3, and 5%. Sorption of Pb on soil mixed with 3%HC increased in heavy metal concentration while 0% HC and 5% decreased in concentration. The removal of Pb by soil mixed with hydrochar was obtained about 93.99(±1.88)%. SEM images showed that the micropores have been developed during HTC reaction which were directly related to the sorption capacity. The average pore diameter of 3% hydrochar mixed with soil was 19 nm while Pb2+ ionic diameter is 0.35 nm. Desorption test showed that desorption of Pb2+ could be neglected, which confirmed that its sorption on hydrochar was stable. In conclusion, hydrochar may play an important role to increase heavy metal removal from the contaminated soil and stabilize the soil in environment.

Keywords: Heavy metal, Hydrochar, Sorption, Food waste, Micropores

Reference:

Bae, S.; Goh, E. S. The Korea Society For Environmental Analysis. 2011, 14, 228-233.

Nunes, C. A.; Guerreiro, M. C. Química Nova. 2011, 34, 472-476.

Mukherjee, A.; Zimmerman, A.; Harris, W. Geoderma. 2011, 163, 247-255.

Figure 1. Effect of hydrochar mixing ratio to soil on lead adsorption and removal rate of lead from the contaminated soil

Introduction to the authors

Ms. Min-Seon Choi pursues M.S. degree in Analytical Chemistry at Seoul Women’s University (SWU). She is interested in conversion of waste to energy source and characterization of its products. Currently, she has been working on optimization of hydrothermal carbonization and physicochemical characterization.

Dr. Sunyoung Bae has obtained Ph.D. from the University of Massachusetts-Lowell in 2002. She had been working at the interdisciplinary research center at the University of North Carolina-Charlotte. In 2008, she was appointed as an assistant professor in the Department of Chemistry at North Carolina A&T State University. Since 2010, she has been working at Seoul Women’s University. Her research approach is to characterize physicochemical properties and interactions in micro-scale using analytical instruments that determines macro-phenomena. Dr. Bae’s research topics include separation and sampling methods for GC, GC-MS, biomass conversion and its characterization. Through some projects that I have conducted, my main role is to integrate fundamental analytical chemistry into a problem-solving solution to a pollution problem. Dr. Bae had been served as a guest editor for Journal of Hazardous Materials (Elsevier), Environmental Monitoring and Assessment (Springer), and Journal of Materials in Civil Engineering (ASCE). Currently, she has been served as an associate editor for Korean Society of Soil and Groundwater Environment and on the editorial board for the Korean Society of Analytical Sciences.