3D Multifunctional N-doped Graphene Foam Inspired by Nature Mussel

Xinhong Song1, Feng Luo2, Xi Chen1*

- College of Chemistry and Chemical Engineering and State Key Laboratory of Marine Environmental Science, Xiamen University, Xiamen 361005, China. Fax: +86 592 2184530; Tel: +86 592 2184530; E-mail: xichen@xmu.edu.cn

- Fujian Research Institute of Metric Science, Fuzhou 350003, China

Introduction and Results:

Inspired by mussel in nature, we introduce a versatile, simple and green but very efficient and industrially approach to build a 3Dimensional N-doped GF(NGF), using biomolecule dopamine as the glue to hold the graphene together. The bio-inspired hierarchical structure provides an efficient 3D network for multifunctional applications due to its high surface area and marvelous low density. Owing to its rich pores inside, the NGF architectures can work as highly qualified candidate in oil adsorption, catalysis, and other technological sustainable applications, in particular, it can absorb amount of the various classes of organic liquids up to 40 to150 times its own weight. The NGF also possesses good electrocatalytic activity; therefore, a sensitive electrochemical sensor has been elaborated to individually or simultaneously determine some biomolecules from their mixture solution.

Figure 1. Two step synthesis of 3D NGF and its digital photograph. Inset: SEM figure of NGF.

Figure 2. (a) Cyclic voltammograms (CVs) of 1.0 mM AA, 1.0 mM DA and 1.0 mM UA in 0.10 M PBS (pH7.4) at N-GF modified GCE at a scan rate of 100 mV/s. (b) Differential pulse voltammograms (DPVs) for 1.0 mM AA, 0.04 mM DA and 0.20 mM UA in a 0.1 M PBS (pH7.4) at bare GCE (A) and N-GF/GCE (B), respectively

Keywords: graphene; ultralight materials: bioinspired; adsorption; electrochemical sensor

Reference:

[1] 1.Lee, H., Dellatore, S. M., Miller, W. M. & Messersmith, P. B. Science, 2007, 318, 426-430.

[2] 2.Yunyong Li, Zesheng Li, Pei Kang Shen, Advanced Materials, 2013, 25, 17, 2474-2480.

Introduction to the authors: Xi CHEN

PhD (1996), Kyoto Institute of Technology

Postdoctoral Fellow (1996), Xiamen University,

Associated Professor (1998), Xiamen University

Professor (2003), Xiamen University

E-mail: xichen@xmu.edu.cn

Tel. +86-592-2184530

Research Interests

Chemo- and Biosensors；

Electrogenerated chemiluminescence；

Food safety analysis；

Miss Xinhong SONG

Student for Ph.D degree, Xiamen University

E-mail: sxhwjsxh@163.com

Tel. +86-592-2184562

Research Interests

Chemo- and Biosensors, Advanced functional materials；

Professor Feng LUO

Fujian Research Institute of Metric Science

E-mail: luofeng 6789@163.com

Tel. +86-591-87804852

Research Interests

Meterage and standards in Chemistry