Quantum dots-based immunosorbent method for the quantitative determination of bisphenol A

Jun Zhang, SuQing Zhao*,Kun Zhang, JianQing Zhou

Department of Pharmaceutical Engineering, Faculty of Chemical Engineering and

Light Industry, Guangdong University of Technology, Guangzhou 510006, China

Abstract: Bisphenol A (BPA) is a ubiquitous environmental contaminant in food products  and aquatic ecosystems. Its endocrine and developmental toxicity presents a serious concern to human health and an effective high-throughput method for  its detection is desirable. In this paper, water-soluble quantum dots (QDs) have been conjugated covalently with BPA antibodies and the conjugate has been utilized in a competitive fluorescence-linked immunosorbent assay (cFLISA). Cd-doped ZnO QDs were functionalized with poly(amidoamine) (PAMAM) dendrimers, as evidenced by ultraviolet absorption spectrum and  fluorescence emission spectra analyses, and this led to their successful transfer into aqueous solution. Biological mass spectrometry demonstrated  that the bisphenol A antibodies were successfully coupled to the water-soluble QDs, and the structures of these conjugates kept intact. The cFLISA method allowed for BPA determination in a linear working range of 20.8–330.3 ng/mL with the limit of detection (LOD) of 13.1 ng/mL. The recoveries of BPA from water samples were from 85.92% to 109.62%. In conclusion, a rapid and sensitive cFLISA was developed by utilizing novel QD coupling method and  validated for use in aquaeous samples.

Fig.1. Calibration curve of cFLISA for BPA. Data are

presented as the means ±SD, (n=3).

Keywords: Quantum dots (QDs); Bisphenol A (BPA); immunosorbent method; competitive fluorescence-linked immunosorbent assay (cFLISA)

*Corresponding authors: sqzhao@gdut.edu.cn, 020-61017546, 0086-15820258676

Acknowledgments:This work was supported by the National Natural Science Foundation of China(No. 41071176, 41271340)