Esterified egg-shell membrane as a novel green sorbent for highly selective uptake of arsenate and speciation of inorganic arsenic

- Ming-Li Chen, Yan Sun, Cui-Bo Gu, Ting Yang, Jianhua Wang*

- Research Center for Analytical Sciences, College of Sciences, Northeastern University, Box 332, Shenyang 110819, China

Introduction and Results: Egg-shell membrane (ESM) is a promising adsorbent for the uptake of heavy metal species. However, carboxylic groups on the surface of ESM are barriers for the adsorption of arsenic. In the present study, the ESM is modified by esterification of carboxylic groups on its surface. The methyl esterified egg-shell membrane (MESM) possesses positive charge within pH 1-9, as shown in Fig.1. As a novel green sorbent material, MESM exhibits a 200-fold improvement on the sorption capacity of arsenate with respect to the bare ESM. Furthermore, the MESM provides an ultra-high selectively of 256:1 for the uptake of As(V) against As(III)(Fig. 2). On this basis, a speciation procedure for arsenate and arsenite is developed with detection by hydride generation atomic fluorescence spectrometry. By loading 4.0 mL sample solution within 0.05-5.00 μg L-1 As(V), followed by elution with 300 μL HCl (1.5 mol L-1), a detection limit of 15 ng L−1 is obtained. A RSD of 3.5% is derived at 0.5 μg L-1. Total amount of inorganic arsenic is achieved by converting As(III) to As(V) and then following the same sorption process.

Keywords: egg-shell membrane; esterification; arsenic speciation; solid phase extraction; hydride generation atomic fluorescence spectrometry

Reference:

1. Fernandez, M. S; Moya, A.; Lopez, L.; Arias, J. L. Matrix Biol. 2001, 19, 793-803.

2. Ishikawa, S.; Sekine, S.; Miura, N.; Suyama, K.; Arihara, K.; Itoh, M. Biol. Trace Elem. Res. 2004, 102, 113-127.

3. Zhang, Y.-J.; Wang, W.-D.; Li, L.; Huang, Y.-M.; Cao, J. Talanta.2010, 80, 1907-1912.

4. Wheelwright, W. V. K.; Easteal, A. J.; Ray, S.; Nieuwoudt, M. K. J. Appl. Polym. Sci.2013, 127, 3500-3505.

Introduction to the authors:

Dr. Ming-Li Chen

Research Center for Analytical Sciences, Box332, Northeastern University, Shenyang 110819, China

Tel: +86-24-83687659; Fax: +86-24-83687659.

E-mail: chenml@mail.neu.edu.cn

Dr. Ming-Li Chen was born in 1979 in Henan, China. She obtained her B.Sc from Department of Chemical Engineering, Zhengzhou University, M.Sc and PhD degree from College of Sciences, Northeastern University, China.

Her current research interest is focused on the exploitation of flow analysis protocols and hyphenation techniques, sample pretreatment (particularly the isolation of trace level of metals from complex sample matrices) and life science analysis.