Nanocarbon materials based electrodes for electrochemical biosensor application

Osamu Niwa1*, Dai Kato1, Kyoko Yoshioka1, Qiang Xue1, Tomoyuki Kamata1, Qiaohui Guo2, Tianyan You2

1National Institute of Advanced Industrial Science and Technology, Biomedical Research Institute, Central 6, 1-1-1 Higashi, Tsukuba, Ibaraki, 305-8566 Japan, 2The State Key Laboratory of Electroanalytical Chemistry, Changchun Institute of Applied Chemistry, Chinese Academy of Sciences, Changchun 130022, P.R. China

Introduction and Results: Top-down and bottom-up nanostructures have been applied for analytical devices including optical and electrochemical sensors. We have been developed nanocarbon based electrodes including sputter deposited nanocarbon films1,2, metal nanoparticle dispersed carbon films3,4 for applying them to various biosensors5-8, or electrochemical detectors for HPLC9-11. Recently, we have fabricated a new carbon film electrode material with thorn-like surface nanostructures to realize efficient direct electron transfer (DET) with enzymes12. Based on this result, we employed carbon nanofiber (CNF) electrodes to immobilize the various enzymes because CNF consists of carbon fibers with a diameter of few hundred-nanometers and can realize various nano-order spaces for enzyme immobilization.

Human cytochrome P450 3A4 (CYP3A4) is deemed to be the most significant enzyme in the P450 families for drug metabolism13,14. CYP3A4 metabolizes more drug molecules than all other isoforms combined and it plays a crucial role in the metabolism of 50 % of clinical drugs. Therefore, it is significant to develop a simple and rapid screening of drug candidates from the viewpoint of metabolism and inhibition by detecting activity change of CYP3A4. Traditionally, the activity of CYP3A4 is determined through the rates of metabolites formation by CYP3A4 require the donation of electrons from NADPH. However, this method is required for expensive reagents and time-consuming. In contrast, electrochemical enzyme sensors based on DET between CYPs and electrodes have been studied in order to realize simple detection of drug metabolite15. We applied CNF modified electrode for evaluating drug metabolism and its inhibition by simply measuring reduction current changes by adding various drugs.

Fig.1. SEM images of CNF at low (left)

and high (right) magnifications.

The SEM images of CNF are shown in Figure 1. We modified CNF on the nanocarbon film formed by unbalanced magnetron sputtering method. The film has wide potential window and low background noise level similar to an ECR nanocarbon film we previously reported1. With our electrode, DET between CNF modified electrode and CYP3A4 was observed at about -0.3 V. We also compared electrocatalytic activity of CYP3A4 co-immobilized with different carbon nanomaterials such as CNF, CNT and carbon black (CB) without modified layer. As a result, CNF and CYP3A4 modified electrode exhibited the most effective reduction current compared with those using other carbon materials (Figure 2). The metabolism of testosterone and quinidine, and its inhibition with ketoconazole were also investigated using CYP3A4 and CNF modified electrode (Figure 3). Efficient drugs metabolism reaction was monitored. Ketoconazole was used to evaluate the inhibition effect on the metabolic activity of CYP3A4. The inhibition efficiency of testosterone metabolism (81.3%) is higher than that of quinidine metabolism (52.8%) as also shown in Figure 3. This could be due to drug-drug interaction between Ketoconazole and quinidine or/and metabolism product 3-hydroxy quinidine.

Fig. 3. Drugs metabolism and inhibition measurements at CNF/CYP3A4

modified carbon film electrodes. (a) testosterone (b) quinidine.

Fig. 2. Comparison of oxygen reduction currents at CYP3A4 and various carbon materials modified electrodes

Keywords: Nanocarbon, Carbon nanofiber, Electrochemical biosensor, Cytochrome P450

Reference: (1) O. Niwa, J. Jia, Y. Sato, D.Kato, R. Kurita, K. Maruyama, K. Suzuki, S. Hirono. J. Am. Chem. Soc., 128, 7144 (2006); (2) J. Jia, D. Kato, R. Kurita, Y. Sato, K. Maruyama, K. Suzuki, S. Hirono, T. Ando, O. Niwa, Anal. Chem., 79, 98 (2007); (3) T. You, O. Niwa, M. Tomita, H. Ando, S. Hirono, Electrochem. Commun., 4 468 (2002); (4) T. You, O. Niwa, T. Horiuchi, M. Tomita Y. Iwasaki, Y. Ueno, Chem. Mater., 14, 4796 (2002); (5) N. Sekioka, D. Kato, R. Kurita, S. Hirono, O. Niwa, Sens. Actuator B., 129, 442 (2008); (6) D. Kato, N. Sekioka, A. Ueda, R. Kurita, S. Hirono, K. Suzuki, O. Niwa, J. Am. Chem. Soc., 130, 3716 (2008); (7) D. Kato, N. Sekioka, A. Ueda, R. Kurita, S. Hirono, K. Suzuki, O. Niwa, Angew. Chem. Int. Ed., 47, 6681 (2008); (8) D. Kato, K. Goto, S. Fujii, A. Takatsu, S. Hirono, S., O. Niwa, Anal. Chem., 83, 7595 (2011); (9) T. You, O. Niwa, M. Tomita, S. Hirono Anal. Chem., 75, 2080 (2003); (10) T. You, O. Niwa, Z. Chen, K. Hayashi, M. Tomita, S. Hirono, Anal. Chem., 75, 5191 (2003); (11) T. Yamamura, M. Hoshikawa, D. Kato, H. Saito, N. Suzuki, O. Niwa, M. Okada. Br. J. Pharmacol. 168, 1088 (2013); (12) A. Ueda, D. Kato, R. Kurita, T. Kamata, H. Inokuchi, S. Umemura, S. Hirono, O. Niwa, J. Am. Chem. Soc., 133, 4840 (2011); (13) S. Joseph, J. F. Rusling, Y. M. Lvov, T. Friedberg and U. Fuhr, Biochem. Pharmacol., 65, 1817 (2003); (14) S. J. Sadeghi, S. Ferrero, G. Di Nardo, G. Gilardi, Bioelectrochemistry., 86, 87 (2012) ; (15) Y. Mie, M. Suzuki and Y. Komatsu, J. Am. Chem. Soc., 131, 6646 (2009).

Introduction to the authors: Osamu Niwa received his B. Eng. degree in 1981, M. Eng. in 1983, and Dr. Eng. in 1990 all from Kyushu University. He joined NTT Laboratories in 1983 and worked in research and development on electrochemical and optical biosensing devices, environmental microfluidic devices and conducting polymers. He was a visiting scholar in Prof. William R. Heineman’s group in the Department of Chemistry at the University of Cincinnati (1990–1991). In 2004, he moved to AIST, and currently he is a Principal Research Manager and Group Leader in Biomedical Research Institute, AIST. His current research interests are electrochemistry of nanocarbon-based materials electrode and their application to chemical sensors and biosensors. He is also interested in various immunosensing device combined with microfluidic devices with SPR, electrochemical and electro-chemiluminescence detections. He has been a president of Society for Chemistry and Micro-Nano Systems (CHEMINAS) from 2012 to 2013 and also steering committee member of International Symposium of Microchemistry and Microsystem (ISMM) from 2012 to 2013. He is also a visiting professor of University of Tsukuba (2005~) and Yamagata University (2013~).